Oxyfuel Gas Cutting (OFC)

OFC – group of oxygen cutting processes that uses heat from an oxygen fuel gas flame to raise the temperature of metal to its kindling temp.

Kindling Temperature – temp at which combustion can begin

- Steel – 1600 – 1800 degrees F

Oxyacetylene cutting – uses oxygen and acetylene

- Most common type of OFC

- Used for cutting and welding

- Cutting is done by preheating the metal with an equal oxygen/ acetylene mixture and then forcing a stream of oxygen through the metal to cut it

Preheat flame required to make a perfect cut is determined by the type of fuel gas used, material thickness, shape, and surface condition

# Lighting the torch

- Set Acetylene at approximately 5psi and the oxygen at 25psi

- Turn on acetylene valve and ignite w/ spark lighter

- Turn the flame up to stop the soot and smoke

- Using just the oxygen valve adjust the flame to a neutral setting

- With the cutting lever depressed, readjust the flame to a neutral setting

# Hand Cutting

  - It is important for the welder to be steady to make a smooth cut.

  - Try getting in position and practicing the cut before lighting the torch

  - Brace the torch w/ the opposite hand of the one used for cutting

  - A slight forward torch angle helps the flame preheat the metal, keeps some reflected flame off the tip, and aids in blowing dirt and oxides away from the cut

  - Inner cone of flame should be kept 1/8 in to 3/8 in from the surface of the plate

  - To start a cut on the edge of the plate, hold the torch slightly pointed away from the edge – as the cut is started, the torch should be rotated back to a slight leading angle

Soft slag – very porous, brittle, and easily removed from a cut

- May be found on some good cuts

Hard slag – attached solidly to the bottom edge of a cut

- Requires a lot of chipping and grinding to be removed

- 30 – 40% more unoxidized iron than soft slag

Slag is found on bad cuts, due to dirty tips, too much preheat, too slow a travel speed, too short a coupling distance, or incorrect oxygen pressure